SB-025

Repairing the DG-5                             12-20-77

The most common problem we have found with the DG-5 to date has been

associated with the RCA type jacks.  The majority of the DG-5's we have

received here for repair have had dirty center pins on the jacks.  The

cause appears to be excessive rosin from soldering running into the center

pin.  The standard repair has been to clean the center pin with solvent.

Another possible problem is a cold solder connection at the RCA jack. You

should also check the interconnection cables for continuity.  This should

take care of about 90% of the DG-5 repairs you will see.

(c) 12277TKC

Downloaded From P-80 International Information Systems 304-744-2253